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Braided Double Insulated FEP/FEP Triple Twisted Flex Product Range: BTFF
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	CABLE CONSTRUCTION
1.  Viscose Rayon braid 
2.  R5F type FEP insulation
3.  180 °C transparent FEP outer insulation 3
4.  Electrolytic tinned flexible concentric rope copper conductor

	APPLICATIONS
This product is designed for use as a pendant drop or table and floor lamps. Approval for rise and fall applications should be confirmed with ourselves prior to adoption.
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Characteristics
	Voltage Rating (U₀/U):
	300 / 500 Vac

	Test Voltage:
	2500 V

	Temperature Range:
	-55 °C ÷ 180 °C

	Short-circuit Temperature:
	160 °C

	Minimum Bending Radius:
	14 x Overall Diameter



	Size Conductor
[mm²]
	Conductor Stranding
[Nº x mm]
	Electrical Resistance
[Ω/Km]

	0.75
	19 x 0.224
	≤ 26.7



	Flexform Product Code
	Size Conductor
[mm²]
	Outer Diameter
[mm]
	Thickness of Jacket
[mm]

	BTFF-403
	3 x 0.75
	5.6 ± 0.5
	≥ 0.60


All versions of this cable can be ordered with a plain or patterned viscose rayon textile braid, available in over 60 colours. Please contact us for a list of available colours.
	Cable Standards
	Low Voltage European Directive No. 2014/35/UE.

	Stranding of Conductor
	Electrolytic tinned flexible concentric rope copper conductor.

	Inner Insulation

Outer Insultation
	R5F type FEP conforming to EN-50363-0 requirements.

R5F type FEP conforming to EN-50363-0 requirements.

	Cable Assembly
	The cores are braided in viscose rayon before being twisted together.


Core Identification		3 Core: Brown  ●  Blue  ●  Green/Yellow  ●
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In order to improve our products, the information contained in this technical datasheet can be changed without notice. Please check periodically with our office, the date and issue number.
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